ARWEI-Premium-Reinstreifer

Data Sheet Portal NKB 23

Tender Specification:

High quality, especially wear-resistant entrance mat, improved absorption of coarse dirt

Application: Indoor and roofed exterior; normal up to extremely strong frequency, suitable for wheelchairs, overall laying, resting distributed burden up to 1,100 kg per 80 sq. cm

Stripe supporting profile: aluminium, V-shaped, every second profile with patented scratching edge; 3 mm ground clearance, uncoupled; sound-absorbing, rinsing, rear ventilated

Cleaning stripes: Needle felt and brush, mix 3/1

Needle felt special ground: 100 % PP; pole density 2,400 g / sq. m; completely needled, no sling ware, minimum contamination; extremely wear-resistant; aluminium profile edges covered halfway through; safe by hidden screw connection; needle felt can be substituted subsequently; colours anthracite, light grey, Copenhagen blue, coconut, special colours on demand; slip resistance R 11 according to DIN 51130

Brush: ARWEI three-way brush; brushes on different levels for an improved absorption of coarse dirt, quieting, colour black, slip resistance R 13 according to DIN 51130

Connection: ARWEI Special Connectors (patented in 1977); therefore easily to roll up, modular construction – no wire or cable connections -, each part can easily be replaced on the spot

Height: 23 mm

Bar distance 3 mm: coarse dirt absorption 6.8 l / sq. m; needle felt walking area 58 cm, 18 scratching edges and 27 brush profiles each m of walking depth

Bar distance 5 mm: coarse dirt absorption 7.7 l / sq. m; needle felt walking area 54 cm, 17 scratching edges and 25 brush profiles each m of walking depth

Angle frames in 25 x 25 x 3 mm are available in aluminium, brass or stainless steel.

Changes in construction or due to material reserved in the course of product maintenance. All specifications are standard dimension without consideration of tolerances contingent upon production.

# Text boxes

ARWEI Special Connectors

Aluminium Profile

Needle Felt

ARWEI Three-          Way-Brush

Scratching Edge