ARWEI-Premium-Reinstreifer

Data Sheet Portal SN 12

Tender Specification:

High quality, especially wear-resistant entrance mat

Application: Indoor and roofed exterior; normal up to extremely strong frequency, passable by shopping trolley, pump truck, car, etc., suitable for wheelchairs, overall laying, resting distributed burden up to 6,500 kg per 80 sq. cm

Stripe supporting profile: aluminium, scratching edges integrated sideways; sound-absorbing

Needle felt special ground: special ground; completely needled; minimum contamination; extremely wear-resistant; safe by hidden screw connection; needle felt can be substituted subsequently; colours anthracite, light grey, blue; beige-brown, green, red, black; slip resistance R 11 according to DIN 51130

Connection: ARWEI Special Connectors; therefore easily to roll up, high slip resistance due to anti-slip function; modular construction – no wire or cable connections -, each part can easily be replaced on the spot

Height: 12 mm

Bar distance: 4 or 6 mm

Angle frame in 15 x 20 x 2 mm is available in aluminium .

Changes in construction or due to material reserved in the course of product maintenance. All specifications are standard dimension without consideration of tolerances contingent upon production.

# Text boxes

ARWEI Special Connectors

Aluminium Profile

Needle Felt

Scratching Edge