ARWEI-Premium-Reinstreifer

Data Sheet Portal SN 17 - locked

Tender Specification:

High quality, especially wear-resistant entrance mat, specially designed with modified connectors and specially constructed angle frame, secured against vertical deformation (applied for a European Patent)

Application: Indoor and roofed exterior; normal up to extremely strong frequency, passable by shopping trolley, pump truck, car, etc., suitable for wheelchairs, overall laying, resting distributed burden up to 10,000 kg per 80 sq. cm

Stripe supporting profile: aluminium, scratching edges integrated sideways; sound-absorbing

Needle felt special ground: 100 % PP; pole density 2,400 g / sq. m; completely needled; no sling ware, minimum contamination; extremely wear-resistant; aluminium profile edges covered halfway through; safe by hidden screw connection; needle felt can be substituted subsequently; colours anthracite, light grey, Copenhagen blue; coconut, special colours on demand; slip resistance R 11 according to DIN 51130

Connection: ARWEI Special Connectors; therefore easily to roll up, high slip resistance due to anti-slip function; modular construction – no wire or cable connections -, each part can easily be replaced on the spot

Height: 17 mm

Bar distance 4 mm: needle felt walking area 72 cm each m of walking depth

Bar distance 6 mm: needle felt walking area 68 cm each m of walking depth

Specially constructed angle frames in 20 x 20 x 3 mm are available in stainless steel.

Changes in construction or due to material reserved in the course of product maintenance. All specifications are standard dimension without consideration of tolerances contingent upon production.

# Text boxes

ARWEI Special Connectors

Aluminium Profile

Needle Felt

Scratching Edge